## Slide 1
7. Catalyst BS13.56
- evaluation of reducing conditions
6. Standard conditions were
established using catalyst BS14.76
10. References and Acknowledgments
5. Measured/calculated parameters
4. The catalysts – preparation and characterisation
3. The catalysts – general remarks
Hydrogen peroxide is a versatile and ‘green’ oxidising agent (the only by-product is water) widely used as a bleaching agent in the paper and textile industries.1 It also finds many applications in the chemical industry, water treatment, semiconductor wafer cleaning and low-cost fuel cell technology.2 However, it is routinely produced on the large scale by the environmentally unfriendly anthraquinone process. Therefore, direct H2O2 synthesis (from gaseous H2 and O2) has emerged as a desirable alternative.3 Flow chemistry and the microreactor technology have been successfully used for this process by several groups.4 Our interest lies in developing an integrated microfluidic process for H2O2 direct synthesis, possessing a minimalised ecological footprint while improving the results described in the literature.
1. Background and objectives
Hage, R. Lienke, A. Angew. Chem. Int. Ed. 2006, 45, 206.
Lane, B.S, Burgess, K, Chem. Rev. 2003, 103, 2457; De Faveri et al, Chem. Soc. Rev. 2011, 40, 1722; Fukuzumi, S. et al, Electrochim. Acta 2012, 82, 493.
Campos-Martin, J. M. et al, Angew. Chem., Int. Ed. 2006, 45, 6962; Edwards, J.K. et al, Science 2009, 323, 1037; Edwards, J.K. and Hutchings, G.J. Angew. Chem., Int. Ed. 2008, 47, 9192; Samanta, C, Appl. Catal. A 2008, 350, 133; García-Serna, J. et al, Green Chem. 2014, 16, 2320;
Inoue, T. et al, Chem. Lett. 2009, 38, 820, Chem. Eng. J. 2010, 160, 909, Fuel Process. Technol. 2013, 108, 8, Chem. Eng. J. doi: doi:10.1016/j.cej.2014.11.019, Catal. Today doi: 10.1016/j.cattod.2014.03.065; Jaenicke, S. et al, Appl. Catal. A 2007, 317, 258, J. Catal. 2010, 269, 302; Voloshin, Y. et al, Catal. Today 2007, 125, 40, Chem. Eng. Sci. 2010, 65, 1028; Turunen, I. et al, Russ. J. Gen. Chem. 2012, 82, 2100.
Blanco-Brieva, G. et al, Chem. Commun. 2004, 1184; Burato, C. et al, Appl. Catal., A 2009, 358, 224; Kim, J. et al, ACS Catal. 2012, 2, 1042; Sterchele, S. et al, Appl. Catal., A 2013, 468, 160; Biasi, P. et al, Ind. Eng. Chem. Res. 2013, 52, 15472; Chung, Y-M. et al, Chem. Commun. 2011, 47, 5705.
This work is supported by WBGREEN – MICROECO (Convention No. 1217714). We are grateful to Dr. Pierre Miquel (Solvay nv) for useful discussions and advice and to Corry Charlier (Unamur) for assistance with the electron microscopy,
Palladium supported on sulfonated polystyrene resins as catalyst for the direct flow synthesis of H2O2
Eduard Dolušić, Aurélie Plas and Steve Lanners
Unit of Organic Chemistry, University of Namur
Namur Medicine & Drug Innovation Center (NAMEDIC), Namur Research Institute for Life Sciences (NARILIS), B-5000 Namur, Belgium
eduard.dolusic@unamur.be
Catalytic systems based on palladium supported on strongly acidic macroreticular polystyrene resins have been described by several groups.5 We started with commercial Amberlyst-15® and loaded it with Pd(II) following the method described by Blanco-Brieva et al. This permitted reaching 2.69 % wt. H2O2 as the maximal concentration when adapting the experimental conditions from Inoue’s work (flow (methanolic working solution) = 10 mL/min, flow (H2) = 1.67 sccm, flow (O2) = 3.33 sccm).4
As particle size of Amberlyst-15® is not convenient for microfluidic applications, we decided to prepare our own catalysts which possess a more
narrow particle size distribution (40 - 80 µm), starting from commercially available Bio-Beads® (polystyrene-divinylbenzene resin).
H2 + O2
H2O2
The reducing conditions significantly affected the catalytic performances. Reduction by MeOH afforded a higher activity in H2O2, but also H2O formation – the latter by H2O2 decomposition and/or other side reactions. A better selectivity was achieved using reduction by H2 in acetone, especially after prolonged treatment (~28 h).
This catalyst batch was then prepared by using H2 as the reducing agent for 28h. We noted that the highest concentration of H2O2 was obtained using 0.5% Pd on Bio-Beads® (average [H2O2 ] = 0.74 % wt.). On the contrary, the selectivity was slightly better when using 1% Pd. As the latter catalyst seemed to have a better recyclability (details not presented), we have chosen it for future work.
50 mg ~ 10 cm of catalyst
0.42 sccm H2, 0.83 sccm O2
50 mL/min of 25 ppm KBr in MeOH (no H3PO4)
ambient temperature
BPRexit 8 bar; system press. 6.5-8 bar
typical result 0.7 % wt. H2O2, S ~50 %, conversion >80 %
best result (cat. amount and all flows tripled) 0.98 % wt. H2O2, S = 63 %, conversion = 94 %
The influence of the catalyst preparation method was investigated, including % of Pd(II) loaded, the immobilisation solvent and the reductive treatment for the conversion to Pd(0).
2. Experimental set up
We have been able to establish optimal conditions for a direct flow synthesis of H2O2 by using Pd supported on sulfonated polystyrene resins as the catalyst. The gas and liquid flow rates, gas ratio and the catalyst amount were optimized, which enabled a further study on the effect of the reducing agent, the reduction time for the preparation of the catalysts, as well as the influence of Pd loading. We have learned to master the reaction conditions, rendering the results more reproducible and easier to interpret. Further experiments are in progress, including kinetic studies, using bi- or trimetallic catalysts and an integration of our system with an H2O2 in-flow concentration system.
Preparation:
- sulfonation of Bio-Beads S-X12®
- Pd immobilisation in a solvent
- reductive treatment (Pd(II) -> Pd(0))
Characterisation :
- titration : resin capacity
- SEM: size distribution
- BET: specific surface area
- porosimetry
- ICP: Pd amount
- XPS: Pd species
- TEM: size of Pd nanoparticles
Reductive treatment:
Catalyst code | Reducing agent | Reduction time (h)
 | Hydrogen balloon-10 mL acetone-RT | 28
 | Hydrogen balloon-10 mL acetone-RT | 3
 | 10 mL refluxing methanol | 28
 | 10 mL refluxing methanol | 3
XPS analysis (catalyst BS 13.63):
338,0 eV
336,2 eV
335,8 eV
2 Pd species : PdII & Pd0
1 Pd species : Pd0
BS xy
%Pd loaded
resin capacity
[meq (H+) / g]
8. Catalyst BS13.56
- evaluation of %Pd loaded
[H2O2] % wt. = m (H2O2) / m (final solution)
Selectivity vs. H2O formation
S = [H2O2] / ([H2O2] + [H2O])
% H2 conversion = ([H2O2] + [H2O])formed / [H2]introduced
9. Conclusion
2H2 + O2 -> 2H2O
2H2O2 -> 2H2O + O2
H2O2 + H2 -> 2H2O